## Slide 1: Experimental challenges of topological insulators: from growth to axion electrodynamics
Carlos M. M. Rosário1, Daniel Brito1, Daniel Sousa1, Daan Wielens2, Martijn Lankhorst2, Tjerk Reintsema2, Sietse Reintsema2, Chuan Li2, Alexander Brinkman2, Sascha Sadewasser1
1 INL – International Iberian Nanotechnology Laboratory, Braga, Portugal
2 MESA+ Institute of Nanotechnology, University of Twente, Enschede, Netherlands

## Slide 2: Topological insulators
Introduction
Topological surface states:
Topologically protected by TRS
Spin-momentum locking
No backscattering
2D TIs (QSHI)
3D TIs
Y. Tokura et al., Nat. Rev. Phys. 1, 126 (2019)
M. Z. Hasan and C. L. Kane, Rev. Mod. Phys. 82, 3045 (2010)
4 ℤ2 topological invariants ()
1 ℤ2 topological invariants ()

## Slide 3: Outline
Experimental challenges of topological insulators
  TIs for novel applications
  TIs for spintronics (Project TopRooT)
  Role in energy-efficient computing
  Topological insulators @ INL (MBE growth and opportunities)
  Experimental challenges of TIs
Topological insulators for axion electrodynamics
  Axion electrodynamics with TIs
  Josephson Junction Arrays (JJA) with TIs
  Some results of the JJAs with TIs
  Experimental challenges

## Slide 4: Experimental challenges of topological insulators
Applications, growth and work in progress @ INL

## Slide 5: Topological insulators
Novel applications
“Typical” electronics
New quantum phenomena
Optoelectronics and plasmonics
Spintronics
Topological p-n junctions
Topological interconnects
FETs
Spin-orbit torque devices
Magnetoelectric effect (new inductor)
THz photodetectors
THz radiation rectifiers
Metamaterials
M. J. Gilbert, Comms. Phys. 4: 70 (2021)
O. Breunig and Y. Ando, Nat. Rev. Phys. 5: 035504 (2017)
Majorana physics
Topological superconductivity
QAH and QSH insulator
Axion electrodynamics
A. Politano et al., APL Mater. 5: 035504 (2017)
Fabrication issues
Intrinsic “doping” by defects
Oxidation of the surfaces
Difficult to gate properly
Low T
Why target devices for spintronics?
Spin-momentum locking of TIs
Already shows promising results at room T
But still in early stage
A lot of fabrication challenges
High potential for high energy efficient electronics
Common problems:
BUT so far there is no outstanding application demonstrated at higher level (metrology with QAH insulators)
TopRooT – Towards topological insulator-based electronic devices for room temperature operation
MSCA ERA Fellowship

## Slide 6: Topological insulators
TIs for spin-orbitronics
Conventional MRAM
STT-MRAM
Magnetic Tunnel Junction (MTJ)
Free layer
Reference layer
Tunnelling Magnetoresistance (TMR)
Parallel
Anti-parallel
Lower TMR
Higher TMR
D. Apalkov et al., Proc. IEEE 104, 1796 (2016)
SOT-MRAM
Q. Shao et al., IEEE Trans. Magn. 57: 800439 (2021)

## Slide 7: Topological insulators
TIs for spin-orbitronics
Q. Shao et al, IEEE Trans. Magn. 57: 800439 (2021)
Spin Hall Effect
Rashba-Edelstein Effect
Charge current density (Je)
Spin current density
(Js)
Idea:
2DEGs with high spin-orbit coupling
Topological insulators
Topological semimetals
Heavy metals (Ta, Pt, W)
SOC
Spin Hall angle:
< 1
>> 1
High potential for topological insulators!
(in principle)
Integration of high-quality TIs in MRAM fabrication process is hard
Limited density of states in TSSs
…
BUT
Integration of TIs with FMs possibly opens up other research routes
Gain knowledge on the fabrication of devices with TIs
HOWEVER
Figure of merit (efficiency)

## Slide 8: Topological insulators
D. Apalkov et al., Proc. IEEE 104, 1796 (2016)
STT
X. Han et al., Appl. Phys. Lett. 118, 120502 (2021)
SOT
STT needs high current through the MTJ to change state – impact on endurance
SOT should allow for more energy-efficient switching and higher endurance
FM
MgO
FM
Magnetization dynamics: Landau-Lifshitz-Gilbert (LLG) equation
Effective field
With STT current
TIs for spin-orbitronics
(SOT is similar)

## Slide 9: Topological insulators
Energy-efficient computing
25 W
1.4 MW
Q. Xia and J. J. Yang., Nat. Mater. 18: 309 (2019)
Artificial Intelligence
Magnetic tunnel junction (MTJ) on a TI (SOT layer)
Spin-momentum locking in TIs
Energy-efficient magnetization switching with SOT
Non-volatile memory devices
Nano-oscillators
Artificial synapses
Artificial spiking neurons
Brain-inspired computing

## Slide 10: Topological insulators @ INL
MBE growth of Bi2Se3
Elements: In, Ga, Bi, Cu, Se
Commonly grown materials:
Bi2Se3, In2Se3, GaSe, CuInSe, …
12 nm of Bi2Se3 on top sapphire (+buffer layers)
Substrates: 2-inch sapphire, Si, GaN, …
Bonus: UHV connection to UHV STM/AFM
Molecular beam epitaxy (MBE)
in-situ RHEED
TEM images by James Peters (INL, Nanostructured materials)
Sapphire
Bi2Se3
Pt
XRD
AFM
Enables growth of Bi2Se3 with good crystalline quality (TEM, XRD) – van der Waals epitaxy

## Slide 11: Topological insulators @ INL
MBE growth of Bi2Se3
Bi2Se3
Other material systems: (Bi,Sb)2Te3 (BST), BiSbTeSe2 (BSTS)
Gating (top and/or bottom gates)
J. Zhang et al., Nature Communications 2, 574 (2011)
BUT slightly lower bandgap of BST when compared to Bi2Se3 (300 meV)
BUT more complex substrates, additional processing steps or liquid gates needed
G. Kunakova et al., Phys Rev Applied 16, 024038 (2021)
(Bi2Se3 nanoribbons on STO)
MBE @ INL:
Limited to selenides
But additional elements available can help (In, Ga, Cu, Se)
Problem: EF in conduction band!
Daniel Brito, PhD thesis, University of Porto (2024)
Surface states contribution is masked by the bulk states
ARPES of Bi2Se3

## Slide 12: Topological insulators @ INL
MBE growth of Bi2Se3
Recipe 2: Buffer layers with In2Se3
Objective: decrease the level of defects – less bulk transport (higher contribution from TSSs)
Recipe 1: Surface treatment
Bi exposure @ 140 °C
3 QL Bi2Se3 growth @ 140 ° C
Evaporation of Bi2Se3 @ 500 °C
Growth of 3 QL Bi2Se3 @ 140 °C
Continue growth of Bi2Se3 @ 310 °C
Problem: EF in conduction band due to self-doping by intrinsic defects (e.g., Se vacancies, twinning)
Better electronic properties (slightly)
Daniel Brito, PhD thesis, University of Porto (2024)

## Slide 13: Topological insulators @ INL
Problem: EF in conduction band due to self-doping by intrinsic defects (e.g., Se vacancies, twinning)
Ga- and Cu-doping of Bi2Se3 during growth
Ga-doping:
Increase of the carrier concentration
Decrease of the mobility
Disappearance of WAL for doped samples
D. Brito et al., J. Appl. Phys. 132, 115107 (2022)
Cu-doping:
Opposite effect: slightly lowers the carrier concentration (BUT not enough to bring EF to bandgap)
Daniel Brito, PhD thesis, University of Porto (2024)
Cu-doped Bi2Se3
Objective: compensate n-type self-doping with deliberate doping with other elements (p-type)
Ga-doped Bi2Se3

## Slide 14: Topological insulators @ INL
Ca-doping of Bi2Se3 by ion implantation
It’s normally considered that TIs require very good crystalline quality to exhibit the topological properties
Ion implantation is another approach to dope the Bi2Se3 thin films (after growth)
P. A. Sharma et al., Appl. Phys. Lett. 105, 242106 (2014)
Collaboration with Marco Peres
From the literature: Ca is a good candidate for doping the Bi2Se3 p-type.
BUT what about the impact on the structural properties?
On the other hand, there is a growing interest in polycrystalline and amorphous topological materials
Provides a wide range of elements as dopants
MSc thesis of Daniel Sousa (UMinho)
Bi2Se3 thin films (30 nm) have been implanted with Ca-ions at 17 keV with different fluence values
Structural characterization (XRD, Raman)
Electrical characterization (ρ, Hall)
Work in progress:

## Slide 15: Topological insulators @ INL
Interfacing Bi2Se3 with trivial materials (Project TopRooT)
2 – 6 %
Efficiency should increase if we find a better solution for the Bi2Se3 transfer!
3.5 %
Microfabrication in the cleanroom
Spin-torque ferromagnetic resonance (ST-FMR) measurement:
Still very far from the expected value!
MSCA ERA Fellowship
Intermediate layer: ??
(in-situ vs. ex-situ)
Problem: oxidation of TI surface in air
Available options:
In-situ deposited capping layers (Se, In2Se3)
In-situ etching before deposition of additional layers
(…)
In collaboration with Spintronics group @ INL

## Slide 16: Experimental challenges of TIs
Growth of TIs by scalable/industry-friendly deposition techniques
Growth of TIs where the topological surface states are accessible at high T
Interfacing TIs with topologically-trivial materials to achieve different functionalities
Fabrication of functional devices based on TIs using standard cleanroom fabrication techniques
Topological properties associated with good quality crystals
Good quality (epitaxial) TIs: MBE
Polycristalline TIs: sputtering
Opportunity for amorphous TIs?
Intrinsic defects of thin film TIs: bulk conductance masks TSSs
Strategies: alloying, gating, doping
Sensitivity of TI surfaces (oxidation)
Problems of intermixing at the interfaces
Strategies needed to preserve TSSs
Sensitivity of TIs (etching)
Fabrication challenges: sophisticated devices at the nanoscale

## Slide 17: Topological insulators for axion electrodynamics
Experimental attempts to measure the Witten effect @ University of Twente

## Slide 18: Axion electrodynamics
Field theory
(Lagrangian formalism)
(Axion term in the Lagrangian density)
Coupling between the E and B fields (magnetoelectric effect)
Spatial or temporal variations of
A. Sekine and K. Nomura, J. Appl. Phys. 129, 141101 (2021)
Daan Wielens, PhD thesis, University of Twente (2021)
Axion
electrodynamics
Topologically-trivial material
TI
= 0
=
Gradient of at the interface
Fine structure constant
Topological magnetoelectric effect

## Slide 19: Axion electrodynamics with TIs
Proposal of an experiment by Nogueira et al.
F. S. Nogueira et al., Phys. Rev. Lett. 121, 227001 (2018)
Type-II Superconductor
TI
= 0
=
A magnetic field can penetrate the SC and create Abrikosov vortices each associated with a magnetic flux :
Abrikosov vortices in a Nb square measured by Scanning SQUID Microscopy
Due to axion electrodynamics at the TI/SC interface:
Every vortex should be associated with a fractional charge
Considering no external charge and one single vortex
Magnetic flux
There is only gradient of along z
+
Uniform B-field along z but only at certain radial points (vortices)
Total magnetic flux = Nv*
Daan Wielens, PhD thesis, University of Twente (2021)
z
How to experimentally probe this charge?
(similar to the Witten effect of a magnetic monopole in a TI)

## Slide 20: Axion electrodynamics with TIs
F. S. Nogueira et al., Phys. Rev. Lett. 121, 227001 (2018)
Aharonov-Bohm-like interference experiment in a Josephson Junction Array (JJA)
Interference of Josephson vortices (vortices in the barrier)
Unpinned vortices move perpendicularly to an external current I
Hole in the JJA creates different paths for the vortices that will pick up different phases in the presence of a B-field
Vortices still carry a quantized flux ()
Phase picked up leads to oscillation of the Ic(B) of the JJA
The phase and thus the oscillation period depend on the charge:
Cooper pairs: 2
Fractional charge:
Small period (t)
Large period (T) = 8t
J. M. Brevoord et al., Nanotechnology 32, 435001 (2021)
Daan Wielens, PhD thesis, University of Twente (2021)
Proposal of an experiment by Nogueira et al.

## Slide 21: Axion electrodynamics with TIs
J. M. Brevoord et al., Nanotechnology 32, 435001 (2021)
TI
SC
Daan Wielens, PhD thesis, University of Twente (2021)
Experiments on Au (instead of TI) show the oscillations of the Ic due to interference of Cooper pairs
Good agreement with the simulated oscillation peaks
(Simulation package for JJAs developed by Martijn Lankhorst)
Measurements on Au reference sample
Experiment needs:
Growth of TI
Deposition of SC
Patterning of SC islands with the right size and distance to form the JJA with the hole
Electrical measurements with B-field at sufficiently low T
Experimental attempts at measuring the Witten effect

## Slide 22: Axion electrodynamics with TIs
J. M. Brevoord et al., Nanotechnology 32, 435001 (2021)
Daan Wielens, PhD thesis, University of Twente (2021)
Good agreement with the simulated oscillation peaks
(Simulation package for JJAs developed by Martijn Lankhorst)
T = 15 mK
Measurements on BiSbTeSe2 (BSTS) flakes
Limitations:
Flakes are too small to allow sufficiently big arrays (nr. of islands) and have a less controllable geometry
Decrease distance between islands to increase Ic and extend the Ic(B) curve to higher fields
(…)
Experiments with MBE- grown (Bi,Sb)2Te3 thin films
No clear observation of the topological effect
Oscillation period due to Cooper pairs is also visible
No clear larger oscillation period from fractional charge
Experimental attempts at measuring the Witten effect

## Slide 23: Axion electrodynamics with TIs
Nb islands: e-beam lithography diameter= 150-200 nm
spacing = 50 nm
Moving to (Bi,Sb)2Te3 (BST) thin films
Tjerk Reinstema, MSc thesis, University of Twente (2022)
Sietse Reinstema, MSc thesis, University of Twente (2022)
Device fabrication:
  very small structures with very small separation distance! (e-beam lithography)
  Device shunting by incomplete lift-off and liftoff “ears”
Extremely low T needed to achieve superconductivity in the JJAs (dilution fridge)
Low critical currents of the JJAs (100s of nA)
Some of the experimental challenges
Experimental attempts at measuring the Witten effect

## Slide 24: Axion electrodynamics with TIs
Moving to (Bi,Sb)2Te3 (BST) thin films
Oscillation period due to the interference of Cooper pairs is clearly measured and agrees very well with the expected value
Device T-BST-014 C
Device T-BST-014 D
Sietse Reinstema, MSc thesis, University of Twente (2022)
Good agreement for several geometries of the arrays and hole
Experimental attempts at measuring the Witten effect

## Slide 25: Axion electrodynamics with TIs
Moving to (Bi,Sb)2Te3 (BST) thin films
Device T-BST-014 C
Device T-BST-014 D
Sietse Reinstema, MSc thesis, University of Twente (2022)
8 × 0.20 G
In a higher field range, other peaks seem to appear, showing a higher period of oscillation of the Ic.
The separation of the peaks is not very consistent, but the average peak difference is compatible with the expected period for 8 times the Cooper pair interference period for device C.
BUT For other devices, the spread is even larger and the average is not consistent with the expected value.
Experimental attempts at measuring the Witten effect

## Slide 26: Axion electrodynamics with TIs
Au reference samples with the same geometry also seem to show similar oscillations with a larger period!
This brings additional questions to the ascription of the oscillations in BST to the fractional charge!
What is the source of the large oscillations?
Moving to (Bi,Sb)2Te3 (BST) thin films
On the other hand, there are other details to be considered:
Charge cancellation from the effect at the bottom interface (TI/substrate)?
Need for (magnetically) gapped surface states to achieve the topological magnetoelectric effect – magnetized TIs (QAH insulator)
(…)
Experimental attempts at measuring the Witten effect

## Slide 27: Summary
Experimental challenges of topological insulators
  Novel applications for TIs: spin-orbitronics to exploitation of novel quantum phenomena
  TIs for energy-efficient SOT-MRAM devices – important role in sustainable AI (project TopRooT)
  Experimental challenges:
    Optimize growth and post-processing of TIs to exploit the topological properties
    Need for good interfacing strategies of TIs with trivial materials
    Need for adaptation of fabrication techniques for topological materials
Axion electrodynamics with TIs
  Experimental attempts with Josephson Junction Arrays on a TI (flakes and thin films)
    Interference pattern observed for Cooper pairs
    So far unsuccessful in observing the fractional charge due to axion electrodynamics
    Further details need to be considered to understand the experiments (e.g., magnetic gap)

## Slide 28: THANK YOU