## Slide 1: 2nd Cycle Integrated Project in Engineering Physics
Magnetoresistive devices for industrial applications: improvement of thermal robustness
Mariana Dinis (ist1102424)
Supervisor: Prof. Susana Cardoso de Freitas
January 2026

## Slide 2: Project Goals: Recap
Project goals
Identify key factors impacting thermal robustness
Compare different TMR stacks
1

## Slide 3: Experimental Work: Samples and their differences
Main Differences
SAF spacer thickness (Ru)
Tunneling barrier thickness
Sensing multilayer materials
AFM Thickness
(pinning layer)
Deposition techniques
Cap Layers
Sample 10252
Sample 10261
Sample 8985
2

## Slide 4: 2kOe setup: Resistance as a function of the applied field
Sample 10252
Sample 10261
Sample 8985
  working temperature
  AP state stability
10261 vs 8985
3
AP state

## Slide 5: 140Oe Setup: Detailed look into samples 10252 & 8985
Sample | Linearity (%)
8985 | 95.9
10252 | 91.7
Sample | 
8985 | 0.06
10252 | 0.56
Sample | 
8985 | 0.06
10252 | 0.56
  Reduced values
  High linearity
Coercivity & Linearity
Magnetic Vortex State
4

## Slide 6: Reversibility Study: Sample 10261
  Similar results
  Differences are within experimental uncertainty, due to sensor-to-sensor variation
Thermal tests after re-annealing
5

## Slide 7: Conclusions and Outlook
Thermal robustness
AFM layer + SAF (reference system)
Vortex Magnetic State
Linearity
Coercivity
Reversibility
Study
Loss of exchange bias
Possible re-pinning
6
Additional Samples
Different measurements
Improved devices

## Slide 8: 2nd Cycle Integrated Project in Engineering Physics
Magnetoresistive devices for industrial applications: improvement of thermal robustness
Mariana Dinis (ist1102424)
Supervisor: Prof. Susana Cardoso de Freitas
January 2026
Questions?