## Slide 1
Multi-Level Magnetic Tunnel Junctions
Author: João Nóbrega
Supervisers: Prof. Dra. Susana Freitas

## Slide 2
Motivation
Need for denser and energy-efficient non-volatile memories
Multi-level MTJs enable more than 2 bit per cell
Spin-Orbit Torque offers reliable and efficient writing
Shape anisotropy enables geometry-controlled magnetic states
Micromagnetic simulations are essential for design and optimization
2

## Slide 3
Magnetic Memories
Ttu
FM
Ttu
TB
FM
FM
Higher Resistence
Lower Resistence
Bottom layer: free
Top layer: fixed
Tunnel magnetoresistance
Reading
Writing
Spin Orbit Torque
3
TB
FM

## Slide 4
Device Fabrication
16 dies per wafer, each containing multiple MTJ devices with geometric variations
Independent bottom and top electrodes for electrical access
Die
5
Step: |  |  | 
Part 1 | 0 | Junction deposition | Materials
 | 1 | 1st DWL lithography | Ta bottom electrode definition
 | 2 | 1st etch by ion milling | 
 | 3 | Resist strip | 
Part 2 | 4 | 1st e-beam lithography (double ellipses) | Magnetic elliptical BE definition & protection
 | 5 | 2nd etch - elliptical BE definition & pad protection | 
 | 6 | 1st passivation AI2O3 | 
 | 7 | Oxide lift-off | 
Part 3 | 8 | 2nd e-beam lithography (junction definition) | Pillar and free layer definition
 | 9 | 3rd etch | 
 | 10 | 2nd Passivation AI2O3 | 
 | 11 | Oxide lift-off | 
Part 4 | 12 | 2nd DWL Lithography | Top electrode definition and BE reinforcement
 | 13 | Metallization | 
 | 14 | Metal lift-off | 

## Slide 5
Mumax3 Simulations – SOT
M
Landau-Lifshitz-Gilbert (LLG)
Effective Field
10

## Slide 6
Conclusions
Extension to more complex geometries
Spin–orbit torque was identified as a suitable writing mechanism
Fabricate the proposed multi-level MTJs
Electrical and magnetic characterization
Optimization of materials and device parameters
Experimental fabrication of the proposed multi-level MTJs
12

## Slide 7
Conclusions
End!
13