## Slide 1
Plastic on Particle Physics: Light yeld and attenuation lenght of plastic scintillators and WLS optical fibers

## Slide 2
Sources of damage to plastic scintillators: Natural ageing and radiation damage
Tile measurement for FCC collider
Photodetectors:
i) PMT detector
ii) SiPM -015c and -1325cs detectors
Light yeld and attenuation lenght of plastic and WLS optical fibers

## Slide 3
Fig 1. Tilecal apparatus – 2D simplistic view of the tilecal detector experience
3
x
y
Colimated radioactive source
Measure fibre
Tile
Photodetector (PMT and SiPM)

## Slide 4
Same system now with Tape
Fig 2. Tilecal apparatus – 2D simplistic view of the tilecal detector experience now with tape
y
x
Tile position in steps: ( 400 step = 1 cm)
4400 < x < 14200
∆x = 200 steps
2900 < y < 6500
∆y = 100 steps
Tile
13800 steps
9000 steps
4800 steps

## Slide 5
Chart: light intensity, no tape, x=9300
| 10 | 9.75 | 9.5 | 9.25 | 9 | 8.75 | 8.5 | 8.25 | 8 | 7.75 | 7.5 | 7.25 | 7 | 6.75 | 6.5 | 6.25 | 6 | 5.75 | 5.5 | 5.25 | 5 | 4.75 | 4.5 | 4.25 | 4 | 3.75 | 3.5 | 3.25 | 3 | 2.75 | 2.5 | 2.25 | 2 | 1.75 | 1.5 | 1.25 | 1 | 0.75 | 0.5 | 0.25 | 0
 | 32.1822 | 39.7333 | 40.7311 | 38.0367 | 37.6611 | 33.82 | 38.3189 | 39.1467 | 39.7133 | 39.4944 | 39.1911 | 38.8956 | 42.6756 | 41.8467 | 42.4522 | 41.0611 | 42.1356 | 40.66 | 38.93 | 42.7411 | 43.5756 | 43.1433 | 46.4522 | 36.0178 | 42.3 | 46.4289 | 44.5489 | 47.72 | 42.4156 | 49.7367 | 45.0611 | 47.1467 | 47.7011 | 48.4567 | 47.9656 | 48.2733 | 47.0722 | 43.6533 | 46.6567 | 42.1667

## Slide 6
Chart: Light intensity, with tape in one side, x=9000
| 10 | 9.5 | 9 | 8.5 | 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
 | 14.5211 | 20.5278 | 19.0089 | 19.5589 | 22.2144 | 18.8689 | 20.8256 | 21.8378 | 19.92 | 24.0511 | 22.1833 | 22.1633 | 17.0633 | 24.4633 | 27.14 | 20.6544 | 23.5333 | 23.4656 | 20.0211 | 24.5556 | 21.8622

## Slide 7
Chart: light intensity, no tape, x=4800
| 10 | 9.5 | 9 | 8.5 | 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
2900 | 34.3189 | 38.85 | 37.6456 | 36.6233 | 39.5767 | 38.6378 | 38.9367 | 36.1233 | 38.6233 | 40.9022 | 38.9011 | 47.2611 | 39.6911 | 37.8567 | 43.4656 | 36.2389 | 45.1267 | 44.3778 | 44.0144 | 41.7667

## Slide 8
Chart: Light intensity, with tape in one side, x = 4400
| 10 | 9.5 | 9 | 8.5 | 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
2900 3100 3300 3500 3700 3900 4100 4300 4500 4700 4900 5100 5300 5500 5700 5900 6100 6300 6500 6700 6900 | 7.2933 | 11.5278 | 13.0533 | 15.3733 | 11.6622 | 13.8922 | 11.8078 | 14.7989 | 15.5756 | 13.1644 | 13.5244 | 17.8733 | 16.5222 | 15.8633 | 15.37 | 18.8289 | 22.6344 | 22.1467 | 19.6067 | 18.6744 | 14.5544

## Slide 9
Chart: light intensity, no tape, x=13800
| 10 | 9.5 | 9 | 8.5 | 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
 | 34.57 | 40.2556 | 41.0522 | 42.5511 | 38.4933 | 44.9589 | 36.5067 | 45.02 | 37.4867 | 41.0189 | 42.3033 | 42.6989 | 45.9367 | 42.3356 | 43.0778 | 45.0644 | 37.7011 | 46.5256 | 49.2756 | 41.76

## Slide 10
Chart: light intensity, with tape in one side, x=13800
| 10 | 9.5 | 9 | 8.5 | 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
 | 21.87 | 19.9244 | 22.7478 | 24.8367 | 21.3811 | 18.8178 | 20.9311 | 22.86 | 21.3556 | 19.7022 | 24.18 | 24.3678 | 22.4444 | 23.7333 | 23.2978 | 22.5433 | 22.1344 | 26.1633 | 23.0089 | 26.9189 | 27.6767

## Slide 11
Chart: light intensity, with tape all around 5mm wide, x=8900
| 10 | 9.5 | 9 | 8.5 | 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
 | 12.2217 | 14.0933 | 17.8917 | 16.4767 | 18.455 | 17.7367 | 19.4767 | 19.1167 | 19.775 | 20.8517 | 21.71 | 18.0083 | 21.215 | 23.3733 | 26.7467 | 27.2183 | 26.8033 | 29.6583 | 26.77 | 38.0283 | 24.9917

## Slide 12
Chart: light intensity, with tape all around 2cm wide, x=8900
| 10 | 9.5 | 9 | 8.5 | 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5 | 1 | 0.5 | 0
 | 10.4144 | 12.0789 | 12.5556 | 12.0667 | 12.0433 | 14.2578 | 15.1356 | 7.8811 | 12.6433 | 12.7944 | 15.61 | 8.6856 | 11.9344 | 10.9622 | 7.2278 | 10.1222 | 11.9211 | 7.9411 | 7.7889 | 13.9433 | 14.2333

## Slide 13: PMT’S noise and signal Coefficient
No Tape | X = 13800 | (0,421 ± 0,002) a.u
 | X = 9300 | (0,420 ± 0,003) a.u
 | X = 4800 | (0,410 ± 0,001) a.u
Tape one side | X = 4400 | (0,158 ± 0,025) a.u
 | X = 9000 | (0,236 ± 0,051) a.u
 | X = 13800 | (0,248 ± 0,062) a.u
Tape all around | X = 8900 (5mm wide) | (0,229 ± 0,052) a.u
 | X = 8900 (2cm wide) | (0,118 ± 0,014) a.u

## Slide 14
Chart: SiPM -1325cs detector y = 6400
| 8 | 7.5 | 7 | 6.5 | 6 | 5.5 | 5 | 4.5 | 4 | 3.5 | 3 | 2.5 | 2 | 1.5
 | 0.55667 | 3.9667 | 5.7333 | 6.2 | 6.1667 | 5.9467 | 5.8 | 5.6833 | 5.7133 | 5.7367 | 6.0233 | 5.9733 | 6.13 | 6.12 | 4.73 | 0.74 | 0.43333 | 0.17667

## Slide 15
Chart: SiPM -1325cs detector, y = 6400

## Slide 16
SiPM -1325cs detector, noise and signal coefficient
First measurement | 0,0088 ± 0,0009 a.u
Second measurement | 0,0091 ± 0,0008 a.u